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	FINE ORGANIC INDUSTRIES LTD

	
	TEST REPORT

	Project No
	
	Issued on
	04.05.2026

	Issued by
	
	Completed on
	05.05.2026

	Representative
	
	Nature of Sample
	Ref Standard
	Batch

	Sample Name
	S 9076
	
	Liquid
	Liquid

	Batch No
	63
	Colour of sample
	Ref Standard
	Batch

	Reference Standard
	BYK 9076
	
	Amber 
	Amber

	Ink Base – Nitrocellulose Polyurethane        

	Testing Parameter
	Violet 23
	Violet 27

	
	Ref Standard
	Finalux 108
	Ref Standard
	Finalux 108

	Grinding (µm)
	< 5 µm
	< 5 µm
	< 5 µm
	< 5 µm

	Colour Shade
	Reference Std
	As per Std
	Reference Std
	As per Std

	Transparency
	Reference Std
	Opaque
	Reference Std
	Opaque

	Color Strength (%)
	100.00
	98-99
	100.00
	100.00

	Viscosity (B4 Cup@26°C)
	21 s
	22 s
	19 s
	20 s

	Adhesion (Tape Test)
	Pass
	Pass
	Pass
	Pass

	Gloss @ 60°
	66.4
	55.7
	7.8
	8.1

	Re-solubility (Rating)
	4
	2
	4
	2

	Separation
	No
	No
	No
	No

	Settling 
	No
	No
	No
	No

	Rating: 1 – Fail, 2 – Poor, 3 – Average, 4 – Good, 5 – Excellent

	Note: Re-solubility tested in Ethyl Acetate + Toluene (50:50).

	Results: Not OK (Gloss and Re-solubility inferior).

	Completed By: Mr. Mohan Yadav

	Authorized By: Dr. Sachin Jagtap
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