|  | FINE ORGANIC INDUSTRIES LTD |  |  |  |
| --- | --- | --- | --- | --- |
|  | TEST REPORT |  |  |  |
| Project No |  |  | Issued on | 04.05.2026 |
| Issued by |  |  | Completed on | 05.05.2026 |
| Representative |  | Nature of Sample | Ref Standard | Batch |
| Sample Name | S 9076 |  | Liquid | Liquid |
| Batch No | 66 | Colour of sample | Ref Standard | Batch |
| Reference Standard | BYK 9076 |  | Amber | Amber |
| Ink Base – Nitrocellulose Polyurethane |  |  |  |  |
| Testing Parameter | Violet 23 |  | Violet 27 |  |
|  | Ref Standard | Finalux 108 | Ref Standard | Finalux 108 |
| Grinding (µm) | < 5 µm | < 5 µm | < 5 µm | < 5 µm |
| Colour Shade | Reference Std | As per Std | Reference Std | As per Std |
| Transparency | Reference Std | Opaque | Reference Std | As per Std |
| Color Strength (%) | 100.00 | 98-99 | 100.00 | 98-99 |
| Viscosity (B4 Cup@26°C) | 21 s | 28 s | 19 s | 22 s |
| Adhesion (Tape Test) | Pass | Pass | Pass | Pass |
| Gloss @ 60° | 66.4 | 58.7 | 7.8 | 9.3 |
| Re-solubility (Rating) | 4 | 2 | 4 | 2 |
| Separation | No | No | No | No |
| Settling | No | No | No | No |
| Rating: 1 – Fail, 2 – Poor, 3 – Average, 4 – Good, 5 – Excellent |  |  |  |  |
| Note: Re-solubility tested in Ethyl Acetate + Toluene (50:50). |  |  |  |  |
| Results: Not OK (Gloss and Re-solubility inferior). |  |  |  |  |
| Completed By: Mr. Mohan Yadav |  |  |  |  |
| Authorized By: Dr. Sachin Jagtap |  |  |  |  |

Re-solubility