|  | FINE ORGANIC INDUSTRIES LTD |  |  |  |
| --- | --- | --- | --- | --- |
|  | APPLICATION TEST REPORT |  |  |  |
| Project Name | Dispersing Additive |  |  |  |
| Sample Name | S 9076 |  | Date Issued: 02.06.2026 |  |
| Batch No | SAW08020626 |  | Completed on: 09.06.2026 |  |
| Reference Standard | BYK 9076 |  | Issued by: Mr. Satish Warghude |  |
| Physical Appearance | Reference Standard |  | Amber to yellow viscous liquid |  |
|  | S 9076 |  | Yellow viscous liquid |  |
| Ink Resin base/Ink System: Nitrocellulose |  |  |  |  |
| Testing Parameter | Violet 23 |  | Violet 27 |  |
|  | Ref Standard | S 9076 | Ref Standard | S 9076 |
| Grinding (µm) | < 5 µm | < 5 µm | < 5 µm | < 5 µm |
| Colour Shade | Reference Std | As per Std | Reference Std | As per Std |
| Transparency | Reference Std | Slightly opaque | Reference Std | As per Std |
| Color Strength (%) | 100.00 | 96-97 | 100.00 | 100.00 |
| Viscosity (B4 Cup@26°C) | 29 s | 33 s | 27 s | 29 s |
| Adhesion (Tape Test) | Pass | Pass | Pass | Pass |
| Gloss @ 60° | 67.1 | 63.6 | 8.8 | 8.5 |
| Re-solubility (Rating) | 3 | 1 | 3 | 3 |
| Separation | No | No | No | No |
| Settling | No | No | No | No |
| Testing Parameter | Carbon Black N 330 |  |  |  |
|  | Ref Standard | S 9076 |  |  |
| Grinding (µm) | < 5 µm | < 5 µm |  |  |
| Colour Shade | Reference Std | As per Std |  |  |
| Transparency | Reference Std | As per Std |  |  |
| Color Strength (%) | 100.00 | 100.00 |  |  |
| Viscosity (B4 Cup@26°C) | 32 s | 37 s |  |  |
| Adhesion (Tape Test) | Pass | Pass |  |  |
| Gloss @ 60° | 41.9 | 42.3 |  |  |
| Re-solubility (Rating) | 3 | 1 |  |  |
| Separation | No | No |  |  |
| Settling | No | No |  |  |
| Re-solubility Rating: 1 – Fail, 2 – Poor, 3 – Average, 4 – Good, 5 – Excellent |  |  |  |  |
| Note: Re-solubility tested in Ethyl Acetate + Toluene (50:50). |  |  |  |  |
| Results: Not OK (Gloss and Colour strength inferior). |  |  |  |  |
| Completed By: Mr. Mohan Yadav |  |  |  |  |
| Authorized By: Dr. Sachin Jagtap |  |  |  |  |

| Re-solubility |  |
| --- | --- |